Hangzhou Yinhu Chemical Co.,Ltd

Providing high-concentration formaldehydeless color-fixing agent for you to confect new type enhanced color-fixing agent.
	Product Code
	Chemical Structure
	Speci(%)
	Applying Range

	HYCF-401
	Linear high molecular weight polymer of DADMAC
	40
	Application in cotton, linen, flat-weaving, there is no color change, excellent lightfastness, and excellent fastness to chlorination.

	
	
	50
	

	
	
	60
	

	HYCF-403
	Polycondensate of Dicyandiamide, organic amine, chlorine
	60
	Application as fixing color of cotton, linen, wool, active and acid dyes

	HYCF-406
	low molecular weight polycondensation of Polyamines, dicyandiamide and chlorine
	50
	Application as color fixing agent  of natural fiber, active, direct and  sulfur dyes

	HYCF-420
	Polycondensate of Organic amines, phenols and chlorine
	50
	Application as Dye-fixing cross-linking agent of active, direct, sulfur dyes. very effective for coat printing.

	HYCF-422
	Net-copolymer of DMDAAC, polyamines and chloride
	50
	Application as color fixing agent of cotton knitted fabric, active and direct dyes, excellent lightfast and rubbing fastness.

	
	
	60
	

	HYCF-425
	Multi polycondensate of Organic amines, chlorine and cationic monomer 
	60
	Application as color fixing agent of acid dyes, particularly effective on the wool fiber.

	HYCF-434
	low-molecular-weight polymer of polyamine and chlorine.
	40±1%
	For modifying cationic ion of fiber,to  increase color fastness and the fibre adsorption of coatings.

	HYCF-436
	Copolymer of DMDAAC, polyamines, organic amines and Chlorine
	40
	Improve the soaping fastness, dry and wet rubbing fastness of active dyes like red.

	
	
	50
	

	
	
	60
	

	HYCF-438
	Cationic modified polycondensate of DMDAAC, polyamines and chlorine
	50±1%
	For the improvement of chlorine resistant, sweat resistant and light fastness of cotton and blend fabric

	HYCF-440
	Copolymer of DMDAAC, unsaturated acylamide monomer, polyamines, DICLO 
	40±1%
	improving the wet rubbing fastness of  active, direct and sulfur dyes 

	HYCF-441
	Cationic modified polycondensate of Dicyandiamide, Polyamines  and Chlorine
	50±1%
	Application as color fixing agent  of cotton, hemp, wool and active, direct, acid dyes.


We offer you producing techinics consultation and excellent service FREELY!

Contact: 0571-85028548.

Add: Floor 12th, Unit 1, Builing 2, Zhongrong Chenshi Garden, 224 Tianmushan Road,Hangzhou,310012,China
Tel: +86-571-8502 8646/8502 8645/8502 8946
Fax:+86-571-8502 8640
URL：www.yinhuchem.com                      E-mail：yinhuchem@yinhuchem.com

